Date:			___________________________________

Trainee:		___________________________________

Trainer:		___________________________________

Service Center: 	___________________________________

Windshield Chip Repair Service

| Prepare for Service | Action / Behavior | Rating |
| --- | --- | --- |
| Wear proper uniform to include the recommended Personal Protective Equipment PPE | Safety Glasses Nitrile Gloves | 1 2 P |
| Use Repair Guide to determine reparability | Place repair guide over damage to determine if repair can be successfully made | 1 2 P |

| Primary Duty and Task | Action / Behavior | Rating |
| --- | --- | --- |
| 1. Prepare the Glass |  |  |
| Clean the glass | Apply glass cleaner directly to the towel Clean around the damage Avoid getting moisture in the damage | 1 2 P |
| Place the mirror | Install the mirror on the inside of the windshield to provide a better view of the damage | 1 2 P |

| Inspect damage with magnification | Inspect damage with magnification to locate hard to see legs and moisture trapped in break | 1 2 P |
| --- | --- | --- |
| Inspection with probe | Use glass probe to inspect damage Look for sensitive legs Look for moisture | 1 2 P |
| Cleaning the pit | Use glass probe to clean the pit Remove loose or broken glass Clean out road debris | 1 2 P |

| 2. Prepare the Equipment |  |  |
| --- | --- | --- |
| Lube lower seal | Use one drop of resin Moisten the whole seal | 1 2 P |
| Lube upper seal | Place small amount of seal lube on finger Completely cover seal | 1 2 P |
| Prepare injector assembly | Loosen guide screw Align threading with guide screw Tighten guide screw fully | 1 2 P |
| Prepare injector assembly for resin | Turn piston back 1-1/2 to 2 turns | 1 2 P |
| Load resin in injector assembly | Insert injector in stand Install 5 drops of resin in injector | 1 2 P |
| Placing white seal on tip of injector | Inspect seal for cracks Place seal in end of injector Press firmly so seal fits snuggly | 1 2 P |
| Adjust resin level in injector | Turn piston down slightly Push resin to the surface of the white seal | 1 2 P |
| Install UV blocker on windshield | Install UV blocker to block ultra violet light from repair area which prevents premature curing of resin | 1 2 P |

| Mounting the injector on the windshield | Turn leveling screws so they just touch the glass Create a slight downward pressure for the injector | 1 2 P |
| --- | --- | --- |
| Creating a seal | Loosen the stand lock bolt and align the injector if needed Turn piston until seal just touches glass, then ½ turn | 1 2 P |

| 3. Executing the repair |  |  |
| --- | --- | --- |
| Create a vacuum | Hold injector body Turn piston back until it stops Hold on vacuum for two minutes | 1 2 P |
| Injecting Resin | Hold injector body Turn piston down slowly Watch in the mirror for the seal to expand slightly | 1 2 P |
| Flexing | Start flexing near the white seal Use firm steady pressure Hold for 5–10 seconds | 1 2 P |
| Inspecting the repair | Look in the mirror Flex around the perimeter of the damage Look for air bubbles and unfilled legs | 1 2 P |
| Secondary Cycles | Repeat vacuum and pressure as needed Flex around the perimeter of the damage | 1 2 P |
| Curing | Attach curing light suction cups to glass Angle light towards damage Let cure for one minute per side | 1 2 P |
| Final Cure | Remove the injector Place curing lamp directly over the impact point Leave on for one minute | 1 2 P |
| Remove the mirror | Remove the mirror while curing Clean any smudge the mirror may have left | 1 2 P |
| Prepping for pit fill | Hold razor at 45 degree angle Remove any resin that has cured | 1 2 P |
| Filling the pit | Place a drop of pit filler just above the impact point Let the resin run into the pit | 1 2 P |
| Placing the film strip | Roll the film strip upward Try not to trap any air bubbles Do not press the film tab down | 1 2 P |
| Curing the pit filler | Place the curing lamp over the film tab Cure for one minute | 1 2 P |
| Scraping the pit | Peel off the film strip Hold the razor blade at a 90 degree angle Run the razor blade back and forth over the cured resin Create a flat smooth surface | 1 2 P |
| Polishing the pit | Place a pea sized drop of polish on the cork Press firmly Polish for 5-10 seconds | 1 2 P |
| Finishing | Clean windshield inside and out Gather all repair tools | 1 2 P |

| 4. Clean the Equipment |  |  |
| --- | --- | --- |
| Cleaning the injector assembly | Remove piston from injector Remove all seals from injector Clean body with alcohol inside and out Clean piston assembly with alcohol Clean all seals with alcohol Dry completely Store in an unsealed zip top bag to allow seals to breathe | 1 2 P |

# Text boxes

Windshield Chip Repair Service

OJT / Practice DTOG

Proficiency Exam